## Slide 1: From New Chemistry to New Materials: Computational and Data-Driven Discovery
Austin Ellis
Department of Chemistry & Biochemistry, CSUN
May 1, 2026

## Slide 2: Outline
Background
  Quasi-atoms and chemical templates
  Density Functional Theory and Crystal Structure Search
  Machine Learning and Deep Neural Networks
Topic 1. Designing Tunable 2D Electrides
  TMX2 and the role of chemical templates.
  Tunable 2D electrides through defect engineering
Topic 2. High Pressure Superconductivity
  Superconductivity in Molecular Hydrides
  Metallization in High-Pressure H2 molecular crystals
Topic 3. Machine-learning Accelerated Materials Discovery
  Chemical-template Guided Superhydride Discovery
  Seitz-invariant ELF Prediction via a 3D CNN
Conclusions

## Slide 3: Quasi-atom: a missing concept in solid compounds
In solid compounds, all local orbitals are born equal.
Notes: Is it important to have a nucleus to have a localized orbital? Orbital isn’t from nucleus, its from the confinement that results from the nucleus. Actually, even if we don’t have an atom, like in the textbook particle in a box problem, we still have discrete localized orbitals as a result of the confinement. In a solid, we have interstitial regions as a result of confinement from other atoms.

## Slide 4: Quasi-atom Chemistry in materials
Na 200 GPa
Li 80 GPa
Bonding
Anti-bonding
Quasi-atom bonds
Quasi-anions
Quasi-molecules
Once occupied, interstitial states become chemically active sites
Overlap creates distinct motifs: quasi-anions, quasi-molecules, and bonding/anti-bonding quasi-atom pairs
Motifs help explain stability, band-gap behavior, and electron transport in dense materials
Miao et al. Angew. Chem. 2016, 56, 972-975
Notes: Many phenomena are puzzling without this concept. But with it, very clear and easy to understand. Bonding STATE, not interaction

## Slide 5: Quasi-atom bonds govern metal structures
Alkali metals adopt BCC
Alkaline metals adopt close packed except Ba (BCC)
Transition metals
  Grps 3&4 HCP  Grps 5&6 BCC 
  Grps 7&8 HCP  Grps 9,10,11 FCC  Grps 12 HCP
Be FCC
Be HCP
Ca HCP
Ca FCC
Sun & Miao, PNAS 2023
The complex pattern of metal structures: a 100-year puzzle
Notes: 100 year puzzle, first metal structure measured by XRD ~100 years ago. Luckily, this physics puzzle can be explained by chemistry. Why Be takes HCP and Ca takes FCC, its because electrons localize in different ways. In Be electron loxalization goes to tetrahedral site, and they form quasi-molecules. In Ca, they push to the octahedral site. In principle, many metals are atom-quasi atom compounds

## Slide 6: Chemical template theory
6
Sun & Miao, Chem 2023, 9, 443–459.

## Slide 7: The ELF and the chemical templates in superhydrides
Electron localization function (ELF) compares local kinetic energy density to a homogeneous gas
High value = localized electrons
Low value = delocalization
Hydrogen atoms assemble in interstitial sites with high electron localization
Sun & Miao, Chem 2023, 9, 443–459.

## Slide 8: Density Functional Theory and Structure Search
First principles (QM)
Provides energies, forces, and electronic structure by solving for electron density
Allows relaxation of structures at target pressures via enthalpy comparisons
CALYPSO searches over lattice vectors and atomic positions to find low-enthalpy structures
Best candidates undergo further calculations and analysis
Notes: Can talk about general method development progress, DFT, CSS, to ML

## Slide 9: Machine Learning vs Deep Learning
Machine Learning
Deep Learning
Tires
Doors
Input
Extract Labels
Train
Predict
Input
Extract + Train
Predict
$
$
Traditional machine learning usually depends on hand-crafted descriptors extracted from inputs
Deep learning maps those representations automatically during training

## Slide 10: Anatomy of a neural network

## Slide 11: AutoGluon and Convolutional Neural Networks
Automated machine learning framework that trains, tunes, and combines multiple models
Useful for feature-based data where input is a set of descriptors
Convolutional neural networks (CNNs) learn spatial patterns from input
In encoder-decoder form, it can transform one spatial field to another
Notes: Make a connection to slide 9

## Slide 12
Topic 1: Designing tunable TMX2 electrides
Sun, Ellis, et al. J. Phys. Chem. Lett. 2024, 15, 6174–6182.

## Slide 13
TMX2 and Chemical Templates

## Slide 14: From Ca2N Electrides to TMDC Catalysts
Electride: material where trapped electrons act as anions
Electrides enable strong H2 activation
Major limitation: Ca2N is highly sensitive to air and water
Solution: Can we engineer electride states in stable monolayer compounds like TMDCs?

## Slide 15: Chemical-template impacts TMDC stability
Metal sublattice retains distinct interstitial localization across 2H, 1T, and 1T’ phases
Larger ELF value at X0 correlates with lower formation enthalpy

## Slide 16
Tunable electrides through defect engineering

## Slide 17: Vacancy engineering creates strong electrides
Only chalcogen vacancies generated interstitial electrons at the defect sites
Quasi-atom states in VS and VS2-MoS2 contribute strongly near the top of the valence bands
Notes: Explain why vacancy, you start with Mo lattice, once occupied by sulfur and forms MoS2, all electride features are gone. (maintains weak electride in center sites, but chemically useless). If we remove a non-metal atom, we might be able to restore the electride property. Vacancies are well-studied experimentally and there are ways to control their concentrations, so the electride property is tunable

## Slide 18: Localized quasi-atom states at S vacancies
Frontier states in both VS and VS2 are spatially localized at the vacancy-centered quasi-atom site
Localized electride states carry substantial charge at vacancy cite

## Slide 19: Vacancy-induced electrides regulate H adsorption
Chalcogen vacancies trap excess electrons
Localized electrons behave as 0D electride states
Electride states tune H binding toward optimal HER
Notes: Its better to show the catalytic process, show the actual catalytic process. Maybe put these at the end, supplemental?

## Slide 20
Topic 2: High Pressure Superconductivity
Zhao, Ellis, et al. Adv. Funct. Mater. 2025, 35, 2415910.
Ellis, et al. J. Phys. Chem. Lett., submitted.

## Slide 21
Superconductivity in molecular hydrides

## Slide 22: Superhydrides hold record superconducting Tc
High-pressure chemistry unveils unique material structures and unusual stoichiometries leading to discoveries of high Tc superhydrides
Notes: Emphasize what superconuctors are, what superhyrides are. Normally we have stoichiometric structure of LaH3, but under pressure we can make structures like this (LaH10). Why do these structures form at all? Conventional understanding can’t explain it.
What are the goals? Room temperature superconductivity is one, very close, some claim it. Second goal, high Tc under lower more MODERATE pressure, ideally ambient pressure

## Slide 23: The ELF predicts superhydride formation
Electron localization function (ELF) compares local kinetic energy density to a homogeneous gas
High value = localized electrons
Low value = delocalization
Hydrogen atoms assemble in interstitial sites with high electron localization
Sun & Miao, Chem 2023, 9, 443–459.

## Slide 24: Structure and bonding in NaKH12
Electron localization at the interstitial sites surrounded by 6 H2 molecules

## Slide 25: Origin of high Tc Superconductivity
Predicted Tc of 245K at 60 GPa
Higher density of H states near E F
strong electron-phonon coupling

## Slide 26: Elongated H2 bonds create interstitial electronic state
Conventional H2 bonding state
Interstitial orbital between H2 units
Interstitial state becomes occupied above ~0.79 Å

## Slide 27: NaK metal sublattice acts as a chemical template
ELF of NaK metal sublattice shows strong interstitial localization
Occupied orbital of sublattice is centered at the same interstitial sites
Orbital persists in full NaKH12 linking neighboring H2 molecules

## Slide 28
Metallization in high pressure H2 molecular crystals
Notes: transition: what if we completely remove the metals? Pure hydrogen is also an important system, people tried to metallize hydrogen system but it required too much pressure. People found that the metallization doesn’t require metallization of the H2 molecules. Maintains molecular structure at onset of metallization

## Slide 29: Competing phases for dense H2 under pressure
Many proposed phases are very close in enthalpy, assigning a “correct” structure is difficult
Representative structures chosen due to agreement with experimental results
B2n
Ama2
Pickard & Needs, Nat. Phys. 2007, 3, 473–476.

## Slide 30: Pressure-driven gap closure in molecular hydrogen
HSE06 functional is more consistent with experimental metallic transition near 425-500GPa
PBE is known to underestimate energy gaps
PBE – standard DFT functional that approximates electron interactions
HSE06 – more accurate, but more expensive functional (exact exchange)

## Slide 31: Interstitial band-edge states drive metallization
B2n 425 GPa
Ama2 400 GPa
In B2n, conduction band minimum forms lobes that bridge neighboring molecules through dense 3D lattice
In Ama2, layered geometry channels charge into sheet-like pathways between molecular layers

## Slide 32
  Topic 3: Machine learning assisted materials discovery
Sun, Ellis, et al. JACS 2025, 147, 40407–40419.
Ellis, Miao. PRX Intelligence, submitted.
Notes: Cover figure, put a more relevant figure?

## Slide 33
Chemical-template guided superhydride discovery

## Slide 34: The ELF predicts superhydride formation
Electron localization function (ELF) compares local kinetic energy density to a homogeneous gas
High value = localized electrons
Low value = delocalization
Hydrogen atoms assemble in interstitial sites with high electron localization
Sun & Miao, Chem 2023, 9, 443–459.

## Slide 35: Chemical template-based discovery workflow
Using the chemical template theory and corresponding 2-step approach greatly reduces the search space and makes superhydride discovery more efficient.

## Slide 36: Predicting formation energy from metal templates
Step 1. training set preparation (DFT)
Step 2. feature engineering
Step 3. ML model training
Notes: Show autogluon logo again

## Slide 37: Screening metal lattices for promising candidates
Step 4. metal lattice candidates
Step 5. metal lattice screening

## Slide 38: Predicting new superhydride structures
Step 6. Search MHn
Workflow based on the chemical template
New structures will be transferred to other MHn and SCC
Allows us to search complex MHn with very large cells
Notes: Now we can search more complex structures with larger cells in a fraction of the time

## Slide 39: Newly identified metal superhydrides
Many new phases appear at non-integer H/M ratios
Newly identified phases have large primitive cells that would’ve been nearly impossible to search with traditional methods

## Slide 40: Superconductivity of novel superhydrides
Estimated Tc values suggest that many of the newly discovered superhydrides are strong high Tc candidates, with 19 above 100 K
Superconductivity is driven mainly by H-dominated high-frequency phonons
Workflow identified 31 new stable metal superhydrides and 13 new structural prototypes
Ca8H46

## Slide 41
Seitz-invariant ELF prediction via 3D CNN

## Slide 42: The ELF can be expensive to calculate
First Principles (QM)
The time required to run a quantum mechanics-based calculation scales cubically with electron count (N)
Machine Learning (ML)
Solution: We can treat the ELF as a 3D image and train a model to predict it directly
Problem: How do we represent our structure?

## Slide 43: Crystal structure representation
SAD is the electron density obtained by freezing atomic charge density at each atom center without allowing their electron clouds to hybridize or relax into bonded states
Since the SAD and ELF have the same grid size, the problem is now an image transformation

## Slide 44: Making the model Seitz-Invariant
Seitz symmetry – Standard notation system for describing the symmetry operations of crystal structures in 3D space groups
Invariance – Property that guarantees the model makes the same prediction even if the crystal structure is rotated or translated according to its symmetry group

## Slide 45: Architecture for a symmetry-aware image transform
+

## Slide 46: Physics-aware loss function
Kendall Loss: An adaptive weighting scheme that automatically learns how to balance the voxel, gradient, and histogram objectives during training, eliminating the need to manually tune loss weights.

## Slide 47: Electron localization function prediction
Model tested on subset of metal lattices
Maxima most relevant to prediction of superhydride structures

## Slide 48: Conclusions
Quasi-atom states and chemical templates provide a framework for understanding the formation mechanism and structure preference of many compounds
In TMX2 monolayers, chemical templates and vacancies create tunable electride behavior and influence H adsorption
Interstitial states help explain strong superconductivity in molecular hydrogen and pressure driven metallization of H2
Template-guided machine learning accelerates discovery, enabling efficient screening of superhydrides and rapid ELF prediction

## Slide 49: Future work

## Slide 50: Acknowledgements
Dr. Miao
Dr. Teprovich
Dr. Lau
Dr. Sun
Dr. Pandit
Samantha Ellis
Friends at CSUN
Department of Chemistry and Biochemistry
College of Science and Math

## Slide 51: 2H-TMDCs Exhibits Weak Electride Character
ELF reveals interstitial localization at centers of Mo triangles
Electride character is a broader materials trend, not an isolated feature of MoS2

## Slide 52
Chemical templates that assemble superhydrides
Interstitial electrons in metal lattices naturally occupy H lattice orbitals
How can we use this phenomenon to predict new superhydrides?

## Slide 53: Interstitial charge grows before metallization
Charge density difference plots show charge redistribution with increasing pressure
Yellow = charge density lost
Cyan = charge density gained
Metallization preceded by redistribution of charge to intermolecular space, not molecular dissociation